[image: image1.png]


      Jinjiang HC Industry Co.,Ltd
Office address: B 602 WANDA BUILDING, MEILING STREET, JINJIANG CITY, FUJIAN, CHINA
TDS-Airlaid Paper

Name of Goods: 80g Airlaid Paper

	No.
	Items
	Unit
	Standard
	Value

	1
	Strength
	N
	2.0±0.5
	2.2

	2
	Whiteness
	/
	≧83
	85

	3
	Basis Weight
	gsm
	80(±5)
	80

	4
	Thickness
	mm
	1mm-1.5mm(±0.2)
	1.3mm

	5
	Moisture
	％
	≦8% or ≦10%
	7%

	6
	Width
	mm
	72mm(±2)
	70mm


                                               Test Date: 2025-12-16
