[image: image1.jpg]



Jinjiang HC Industry Co.,Ltd.

	
	Untreated Fluff Pulp Specification

	
	SPECIFICATION:-
	Roll Width:508,
	O D : 1200mm , I D : 76 mm
	

	
	Pulping Process
	Kraft

	
	Bleaching Process
	ECF

	
	Wood Species
	Southern Pine


Typical Properties

Average Fiber Length

	FQA Length Weighted (mm)
	2.4

	Kajaani Length Weighted (mm)
	2.7

	Basis Weight (g/m2)
	765

	Caliper (mm)
	1.27

	Density (g/cc)
	0.55

	Mullen (kPa)
	

	No. 1, 3, 8 Machine
	1100-1300

	Moisture (%)
	8.0

	Extractives (%)
	0.03

	Brightness (ISO)
	88.0

	PH range
	5.0-6.5

	Kamas Energy (k Wh/ton)
	26-29

	Fiberization (%)
	>95.0

	Specific Absorption (sec/g)
	<0.75

	Specific Capacity (g/g)
	9.5


Packaging

	Roll Width (cm)
	25 – 152

	Roll Diameter (cm)
	115 – 152

	Core Diameter (cm)
	7.6


